## Slide 1
Influence of different chloride ion
concentration on corrosion of rebar
菂
Qingrui Wang
2017.09.21

## Slide 2
First
Second
Third
Last
Introduction
Raw materials
and equipment
Results and analysis
conclusion
outline

## Slide 3
Introduction

## Slide 4
Introduction
Reinforced concrete is the most commonly used building material, however, the most important factor affecting its service life is the corrosion of steel bars。Therefore, it is of great significance to study how to avoid the corrosion of steel bars.
In this experiment, we mainly study the corrosion of rebar in chloride ion environment.

## Slide 5
这里填写文字内容这里填写文字内容
这里填写这里填写文字内容
这里填文内容里填写文字内容
1.The reinforcing bars were soaked in six groups of saturated calcium hydroxide solutions with chloride concentrations of 0.02%, 0.04%, 0.06%, 0.12%, 0.25% and 0.5%.
Introduction
2.Every week using an electrochemical workstation,obtain the the Tafel curve and other electrochemical data.
3.Analyzing its electrochemical data and appearance changes can draw the conclusion

## Slide 6
Raw materials and equipment

## Slide 7
Raw materials and equipment
calcium hydroxide
distilled water
sodium chloride
Q235 reinforcement

## Slide 8
Raw materials and equipment
1.Electrochemical workstation
2.Electronic balance
3. Thermostat water bath

## Slide 9
Raw materials and equipment
1
2
3
4
5
6
Prepare six groups of solutions with different chloride concentrations
(EIS)Electrochemical impedance spectroscopy
Linear polarization curve
Tafel curve
Experiments at different temperatures
Draw with Origin

## Slide 10
Results and analysis

## Slide 11
Results and analysis
time
1
Change
the solution
The first week
The third week
The fifth week
The eighth week
The chloride concentration was 0.02%
Nyquist

## Slide 12
Results and analysis
time
1
Linear polarization curve
Change
the solution
The first week
The third week
The fifth week
The eighth week
The chloride concentration was 0.02%

## Slide 13
1
Tafel curve
Change
the solution
The first week
The third week
The fifth week
The eighth week
The chloride concentration was 0.02%
time
Results and analysis

## Slide 14
1
Appearance change
The change of steel bar and solutions from first week to the eighth week.
time
Results and analysis

## Slide 15
concentration
2
The eighth cycle
The first cycle
Results and analysis
Nyquistc

## Slide 16
2
concentration
Tafel curve
Results and analysis
The eighth
cycle
The first
cycle

## Slide 17
2
The first cycle
The fifth cycle
concentration
Results and analysis
Appearance change
The third cycle
The eighth cycle

## Slide 18
2
concentration
Results and analysis
Appearance change
The fifth cycle
The eighth cycle

## Slide 19
2
The fifth cycle
The eighth cycle
concentration
Results and analysis
Appearance change

## Slide 20
temperature
3
20℃
30℃
40℃
50℃
Results and analysis
Nyquist
The chloride concentration was 0.12%

## Slide 21
3
The chloride concentration was 0.12%
temperature
Results and analysis
Tafel curve

## Slide 22
3
temperature
Results and analysis
Appearance change
The appearance change of steel bar and solutions from 20℃ to 50℃

## Slide 23
conclusion

## Slide 24
conclusion
1
2
3
With the passage of time, the ability of reinforcing steel to resist corrosion becomes weaker, and the corrosion of reinforcing steel is more and more serious
Time
The higher the chloride concentration is, the weaker the resistance of steel to corrosion is, the worse the corrosion of reinforcing steel is
Concentration
With the increase of temperature, the weaker resistance to corrosion of steel, corrosion becomes more serious
Temperature

## Slide 25
Thank you