## Slide 1
Nucleation and control in the solidification process of Al-Bi monotectic alloy
Name:Zhang Youkang
Major:Material forming and control engineering
Graduate University:Qilu University of Technology

## Slide 2
CONTENTS
01
Introduction of the monotectic alloy
02
Experiment Content
03
Analysis and Conclusion

## Slide 3
01
Introduction of the monotectic alloy
Characterized by a liquid miscibility gap
Al-Pb monotetic alloy is an engine bearing material
Zn-bi alloys have excellent electrochemical properties
It is difficult to prepare homogeneous alloy due to the existence of liquid phase separation

## Slide 4
02
Experiment Content
Experiment object：Al-Bi montectic alloy
Process：Choose three different compositions Al-Bi
alloy
Add different ratios of Al-5Ti-1B grain refiners
0%、0.1%、0.2%、0.5%
Add the microalloying element Sn, Cu and Si
Analysis：The effect of adding Al-5Ti-1B and microalloying
elements on the solidification of Al-Bi alloy was
investigated by solidification curve and microstructure
observation

## Slide 5
03
Analysis and Conclusion
The influence of Al-5Ti-1B addition on solidification nucleation of Al-Bi alloy
The solidification curve of Al95Bi5 adds a different ratio of Al-5Ti-1B（a）The whole solidification（b）The process of monotectic reaction
Metallographic photographs of Al-Bi alloy with different ratio of Al-5Ti-1B（a）0%Al-5Ti-1B（b）0.1%Al-5Ti-1B（c）0.2%Al-5Ti-1B（d）0.5%Al-5Ti-1B

## Slide 6
The solidification curve of Al92Bi8 adds a different ratio of Al-5Ti-1B（a）The whole solidification（b）The process of monotectic reaction
Metallographic photographs of Al-Bi alloy with different ratio of Al-5Ti-1B（a）0%Al-5Ti-1B（b）0.1%Al-5Ti-1B（c）0.2%Al-5Ti-1B（d）0.5%Al-5Ti-1B
03
Analysis and Conclusion

## Slide 7
The solidification curve of Al84Bi16 adds a different ratio of Al-5Ti-1B（a）The whole solidification（b）The process of monotectic reaction
Metallographic photographs of Al-Bi alloy with different ratio of Al-5Ti-1B（a）0%Al-5Ti-1B（b）0.1%Al-5Ti-1B（c）0.2%Al-5Ti-1B（d）0.5%Al-5Ti-1B
03
Analysis and Conclusion

## Slide 8
03
Analysis and Conclusion
The influence of microalloying elements Sn, Cu and Si addition on the solidification process of Al92Bi8 alloy
The solidification curves of (Al0.92Bi0.08)99Sn1、(Al0.92Bi0.08)99Cu1、(Al0.92Bi0.08)99Si1 （a）The whole solidification（b）The process of monotectic reaction
The metallographic photographs: (b)、(Al0.92Bi0.08)99Sn1、(c)、(Al0.92Bi0.08)99Cu1、(d)、(Al0.92Bi0.08)99Si1

## Slide 9
03
Analysis and Conclusion
The addition of Al-5Ti-1B makes Al-Bi alloy nucleation undercooling degree decreases, and the addition of Al-5Ti-1B release TiB2 as the heterogeneous nucleation point, changing the mode of grain growth, change the form of second phase particles precipitate Bi, refine the grain size.
The addition of Sn, Cu and Si elements in Al-Bi alloy can change the size of the second phase Bi particle, Sn can reduce Bi particle size, Cu and Si increases Bi particle size.

## Slide 10
Thanks！