## Slide 1: Self-Introduction
National material service safety science center
2017.9.21
Li Dan

## Slide 2: Paper title Correlation between Corrosion Behavior and Microstructure of Precipitated Phases in AZ91 Magnesium Alloy with Rare Earth Addition
Testing methods:
SEM/EDS/TEM microstructure of AZ91 magnesium alloy
LSCM/SPM corrosion behavior of precipitated phases
HRTEM/Peak-Force KPFM combination mechanism and potential difference between matrix and precipitated phases
Material : AZ91 Magnesium alloy
Rare earth :
yttrium (Y)
misch metal of lanthanum and cerium (La,Ce)
Testing sample:
AZ91 magnesium alloy
AZ91+0.3% Y
AZ91+0.9% Y
AZ91+0.4%(La,Ce)
AZ91+1.0%La,Ce)

## Slide 3: content
Ⅰ. Microstructure
Ⅱ. Electrochemistry
Ⅲ. Corrosion behavior
ⅰ. macroscopic corrosion morphology(LSCM)
ⅱ . microcosmic corrosion morphology(SPM)
Ⅳ. Correlation between corrosion behavior and microstructure of precipitated phases
ⅰ. Potential difference between matrix and precipitated phases
ⅱ . Interface combination mechanism between matrix and precipitated phases
Ⅴ. Conclusions

## Slide 4: Ⅰ. Microstructure
a)
b)
Second phase:
β-Mg17Al12
AlMn
Matrix:
α-Mg
AZ91
a)
b)
β-Mg17Al12
Rare earth phases
AZ91+Y
a)
b)
Rare earth phases
β-Mg17Al12
AZ91+(La,Ce)
Results:
AZ91 : α-Mg/β-Mg17Al12/AlMn phases
AZ91+Y: α-Mg/β-Mg17Al12/AlY phases/AlMnY phases
AZ91+(La,Ce): α-Mg/β-Mg17Al12/ Al+(La,Ce) phases/AlMnCe phases
fcc: Al2Y
tetragonal primitive: Al2Y3、Al10Mn2Y
bcc: Al4(La,Ce)
body-centered tetragonal:Al8Mn4Ce

## Slide 5: Ⅱ. Electrochemistry
Testing method: polarization curve test and hydrogen evolution test
Testing results(corrosion degree):
AZ91> AZ91+(La,Ce) > AZ91+Y

## Slide 6: Ⅲ. Corrosion behavior
ⅰ. macroscopic corrosion morphology(LSCM)
Corrosive medium: 3.5%NaCl
Under solution: 60 min
a)
c)
AZ91
a)
b)
AZ91+Y
a)
b)
AZ91+(La,Ce)
Results:
AZ91 : general corrosion
AZ91+(La,Ce): matrix around rare earth phases
AZ91+Y: matrix around rare earth phases
localized corrosion

## Slide 7: Ⅲ. Corrosion behavior
ⅱ . microscopic corrosion morphology(SPM)
Corrosive medium: 0.01mol/L NaCl
a)
b)
c)
e)
d)
f)
AZ91
a)
b)
c)
d)
e)
f)
AZ91+Y
a)
c)
d)
f)
a)
c)
AZ91+(La,Ce)
Results:
matrix around rare earth phases was corroded seriously

## Slide 8: Ⅳ. Correlation between corrosion behavior and microstructure of precipitated phases
ⅰ. Potential difference between matrix and precipitated phases
Testing method: Peak-Force KPFM(SPM)
a)
L1
L2
b)
L2
L1
c)
141mv
338mv

## Slide 9: Ⅳ. Correlation between corrosion behavior and microstructure of precipitated phases
ⅰ. Potential difference between matrix and precipitated phases
α-Mg & precipitated phases | β | AlMn | Bulk phases | Needle-like phases | Rod-like phases
AZ91 | 141mV | 338mV | ------ | ------ | ------
AZ91+Y | 151mV | ------ | 399mV | ------ | ------
AZ91+ (La，Ce) | 168mV | ------ | 379mV | 430mV | 412mV
Results:
α-Mg & β-Mg17Al12 around 150mv
α-Mg & rare earth phases 340mv‾430mv
Higher potential difference, more seriously of corrosion degree

## Slide 10: Ⅳ. Correlation between corrosion behavior and microstructure of precipitated phases
ⅱ . Interface combination mechanism between matrix and precipitated phases (HRTEM)
a)
b)
（0）
（101）
（0）
[011]
c)
FFT
d=0.2382nm
d=0.2415nm
（0）
（101）
d)
Inver-FFT

## Slide 11: Ⅳ. Correlation between corrosion behavior and microstructure of precipitated phases
ⅱ . Interface combination mechanism between matrix and precipitated phases (HRTEM)
AZ91 |  | AZ91+Y |  | AZ91+(La,Ce) |  | 
β | AlMn phases | Al2Y | Al10Mn2Y | Al4(La,Ce) | Al4(La,Ce) | Al8Mn4Ce
semi-coherent | non-coherent | non-coherent |  | semi-coherent interface | non-coherent | 
Results:
α -Mg & β-Mg17Al12 semi-coherent
α-Mg & rare earth phases non-coherent
Interface energy: non-coherent>semi-coherent
Higher interface energy, more easily to induce corrosion behavior

## Slide 12: Ⅴ. Conclusions
ⅰ. Corrosion resistance enhanced after rare earth addition;
ⅱ. Although heavily corrosion occurred around rare earth phases, general corrosion of alloys was reduced.
ⅲ. Matrix around rare earth phases is more easily to corrosion because of higher interface energy and higher potential difference.

## Slide 13: Thank you!